ISSN  1999-8716

Diyala Journal

of Engineering Sciences

Printed in Iraq

Vol. 01 , No. 01 , pp. 46-55 , December 2008

Optimizing The Process of Resistance Spot Welding For 2014 – O Aluminum Alloy Sheet

Latfe Y. Zedan1 and Naife A. Talib2

(1,2) Collage of Eng. – Diyala University

(Received:13/5/2008 ; Accepted:13/9/2008)

ABSTRACT - There is a strong interest in the use of aluminum alloy sheet for vehicle applications, particularly the body, where resistance spot welding is the principle joining method. The resistance spot welding (R.S.W) quality has a great effected by the process variable such as, welding current, welding time, and electrode pressure beside other variable such as material thickness and type and electrode diameter.

In this work the effect of process variable on welding quality was investigated. Trials were conducted on 1.2 mm thick 2014 – O aluminum alloy sheet. The tensile shear strength was used as primary index of welds quality. Experimental investigation show that the best current is 45 KA, best time is 10 cycle, and electrode pressure of 3 KN .

Key Words: Spot Weld, Aluminum Alloy Sheet, Shear Strength, Resistance spot Welding

1- THE AIM OF THIS WORK

Improving welds quality by optimizing process variable of spot welds in aluminum alloy sheet.

2- INTRODUCTION

The need to reduce vehicle weight, improve fuel economy and reduce exhaust emissions has led to increased materials such as aluminum alloys (1).While the space frame concept has been claimed as being a cost – effective way of achieving a high – performance vehicle structure, it remains suited to low – volume manufacture. Aluminum alloys have found applications in the more classical design of high volume vehicles (2).Resistance spot – welding