ISSN  1999-8716

Diyala Journal

of Engineering Sciences

Printed in Iraq

Vol. 01 , No. 01 , pp. 110-121 , December 2008

THE EFFECT OF LASER SURFACE HARDENING ON THE WEAR AND FRICTION CHARACTERISTICS OF ACICULAR BAINITIC DUCTILE IRON

kh. m. adel1, A.S. Dhia2 , and M. J. Ghazali 3

1&2faculty of Engineering, university of diyala

3Department of Mechanical and Materials Engineering, Faculty of Engineering, University Kebangsaan , Malaysia.

(Received:7/9/2008 ; Accepted:8/11/2008)

ABSTRACT - Nd-Yag (Neodymium Yttrium) pulsed wave laser has been used to modify and refine the surface microstructure of acicular bainitic ductile iron. The wear characteristics evaluated by adhesion and abrasion wear tests while friction characteristics evaluated by using strain gauge technique of the laser processed and unprocessed (as-cast) specimens were studied. The wear resistance and friction coefficient of laser processed samples are significantly enhanced by their refined bainitic microstructures and improved hardness in the melted and resolidified layer. Cross-sectional optical and scanning electron microscope have been used to study the microstructure and wear mechanism of the laser processed and unprocessed surfaces while X-Ray diffraction technique has been used to study and estimate the metallurgical phases. All specimens treated by laser showed wear and friction resistance higher than as-cast specimens at all loads, sliding speeds and sliding times used in this research work.

Keywords: laser surface hardening, wear& friction characteristics, acicular bainitic ductile iron.